Appendix 1. Chemical composition of selected grains of characteristic microphases of noble metals in zones I and II of the sample

| MF | Formula/ system | Sum | Chemical composition of phases |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Fe | Ni | Cu | Au | Ag | Pt | Pd | Pb | Bi | As | Se | S |
| Zone I |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5а | Pt(As,S)2-х | 99.25 | 2.85 | 0.41 | 2.42 | < b.d.l. | < b.d.l. | 53.63 | < b.d.l. | < b.d.l. | < b.d.l. | 37.54 | < b.d.l. | 2.40 |
|  |  |  | 5.39 | 0.74 | 4.02 | < b.d.l. | < b.d.l. | 29.03 | < b.d.l. | < b.d.l. | < b.d.l. | 52.91 | < b.d.l. | 7.91 |
| 5б | PdS | 101.85 | 6.01 | 3.98 | 2.17 | < b.d.l. | 1.30 | 1.44 | 62.10 | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | 24.85 |
|  |  |  | 6.78 | 4.27 | 2.15 | < b.d.l. | 0.76 | 0.46 | 36.76 | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | 48.82 |
| 5б | Pt-phase* | 101.08 | 28.49 | 3.62 | 18.77 | < b.d.l. | < b.d.l. | 15.18 | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | 35.03 |
|  |  |  | 25.04 | 3.03 | 14.50 | < b.d.l. | < b.d.l. | 3.82 | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | 53.62 |
| Zone II |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 5г | Au* | 107.15 | 11.22 | 6.77 | 4.28 | 59.41 | 4.97 | < b.d.l. | 4.15 | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | 16.34 |
|  |  |  | 15.7 | 9.01 | 5.26 | 23.56 | 3.6 | < b.d.l. | 3.05 | < b.d.l. | < b.d.l. | < b.d.l. | < b.d.l. | 39.82 |
| 5г | ~PdAsBi | 102.48 | 13.96 | 10.51 | 3.03 | 1.75 | 2.19 | 2.81 | 31.83 | 1.34 | 12.27 | 7.18 | < b.d.l. | 15.61 |
|  |  |  | 16.98 | 12.16 | 3.24 | 0.60 | 1.38 | 0.98 | 20.32 | 0.77 | 3.99 | 6.51 | < b.d.l. | 33.07 |
| 5д | (Pt,Pd)AsS | 100.06 | 6.37 | 1.64 | 4.94 | < b.d.l. | < b.d.l. | 37.82 | 7.46 | < b.d.l. | 0 | 31.15 | < b.d.l. | 10.68 |
|  |  |  | 9.25 | 2.27 | 6.31 | < b.d.l. | < b.d.l. | 15.73 | 5.69 | < b.d.l. | 0 | 33.73 | < b.d.l. | 27.03 |
| 5д | ~Pd2(Bi,As) | 94.55 | 1.12 | 0.44 | 1.43 | < b.d.l. | 1.61 | < b.d.l. | 39.31 | < b.d.l. | 44.2 | 6.10 | < b.d.l. | 0.34 |
|  |  |  | 2.72 | 1.02 | 3.05 | < b.d.l. | 2.02 | < b.d.l. | 50.06 | < b.d.l. | 28.66 | 11.03 | < b.d.l. | 1.44 |
| 5д | Ni-Pd-As-S | 95.19 | 13.52 | 16.82 | 3.71 | < b.d.l. | 5.21 | < b.d.l. | 21.54 | < b.d.l. | 6.29 | 13.24 | < b.d.l. | 14.86 |
|  |  |  | 16.05 | 19 | 3.87 | < b.d.l. | 3.20 | < b.d.l. | 13.42 | < b.d.l. | 2.00 | 11.72 | < b.d.l. | 30.73 |
| 5е | Cu-Pb-Bi-S | 100.75 | 3.09 | 0.40 | 9.50 | < b.d.l. | 3.59 | < b.d.l. | < b.d.l. | 55.18 | 13.31 | < b.d.l. | 3.91 | 11.77 |
|  |  |  | 5.58 | 0.69 | 15.08 | < b.d.l. | 3.36 | < b.d.l. | < b.d.l. | 26.86 | 6.42 | < b.d.l. | 4.99 | 37.02 |
| 5ж | Pt(As,S)2 | 92.15 | 1.58 | 0.56 | 1.25 | < b.d.l. | < b.d.l. | 54.19 | 1.54 | < b.d.l. | < b.d.l. | 28.33 | < b.d.l. | 4.70 |
|  |  |  | 3.24 | 1.09 | 2.25 | < b.d.l. | < b.d.l. | 31.76 | 1.66 | < b.d.l. | < b.d.l. | 43.24 | < b.d.l. | 16.76 |
| 5ж | PdxBi1±y | 99.32 | 1.81 | 0.52 | 1.11 | 1.57 | 1.81 | 2.16 | 32.77 | < b.d.l. | 54.7 | 2.14 | < b.d.l. | 0.73 |
|  |  |  | 4.53 | 1.24 | 2.44 | 1.11 | 2.34 | 1.55 | 43.04 | < b.d.l. | 36.58 | 3.99 | < b.d.l. | 3.18 |
| 5з | Ni3(Pb,Bi)2S2 | 96.93 | 4.62 | 20.79 | 1.82 | < b.d.l. | 0.75 | < b.d.l. | 0.69 | 15.42 | 39.78 | < b.d.l. | 1.47 | 11.58 |
|  |  |  | 7.36 | 31.52 | 2.55 | < b.d.l. | 0.62 | < b.d.l. | 0.58 | 6.62 | 16.94 | < b.d.l. | 1.66 | 32.15 |

Note. Compositions expressed in wt.% and in at.% are in the first and second rows for each phase, respectively. MF - micrograph of the phase in Fig. 5. The detection limit was 0.4–0.5 wt.% for Au, Pt, Pb and Bi and 0.1–0.2 wt.% for the remaining elements. b.d.l. – below detection limit. * The presence of Pt phase and native Au was suggested based on the high content of Pt (15.18 wt.%) and Au (59.41 wt.%) in the analysis, respectively.