Appendix 3. The average composition of solid solutions of the Cu-Pb-Bi-S, Cu-Pd-Bi-S and Cu-Ag-Bi-Pb-As-S systems and unknown phases of the Ag-Pb-Bi-S and Ag-Ni-Bi-S systems1

| Fig. 62 | Sum | Average composition of solid solutions |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Fe | Ni | Cu | Ag | Pd | Pb | Bi | Se | S |
| Cu-Pb-Bi-S |  |  |  |  |  |  |  |  |  |  |
| i | 97.18 | 2.34 | 0.32 | 19.27 | 2.28 | b.d.l. | 31.30 | 26.72 | 2.76 | 12.20 |
|  |  | 3.93 | 0.51 | 28.44 | 1.98 | » | 14.17 | 11.99 | 3.28 | 35.69 |
| i | 99.61 | 4.42 | 0.76 | 18.16 | 2.30 | » | 46.77 | 9.58 | 3.19 | 14.42 |
|  |  | 6.82 | 1.12 | 24.62 | 1.84 | » | 19.44 | 3.95 | 3.48 | 38.74 |
| o | 95.9 | 3.94 | 1.70 | 20.00 | 2.00 | » | 34.84 | 16.37 | 2.77 | 14.29 |
|  |  | 6.08 | 2.50 | 27.13 | 1.60 | » | 14.49 | 6.75 | 3.02 | 38.42 |
| l | 99.7 | 3.76 | 0.49 | 21.92 | 1.52 | » | 30.94 | 25.50 | 2.65 | 12.92 |
|  |  | 5.89 | 0.73 | 30.19 | 1.23 | » | 13.07 | 10.68 | 2.94 | 35.27 |
| l | 100.21 | 4.49 | 1.13 | 23.77 | 2.32 | » | 29.14 | 23.64 | 2.56 | 13.17 |
|  |  | 6.74 | 1.61 | 31.38 | 1.80 | » | 11.80 | 9.49 | 2.72 | 34.46 |
| o | 97.86 | 4.15 | 0.59 | 19.06 | 1.72 | » | 41.42 | 14.24 | 2.85 | 13.82 |
|  |  | 6.54 | 0.89 | 26.42 | 1.40 | » | 17.61 | 6.00 | 3.18 | 37.96 |
| o | 96.93 | 4.31 | 2.68 | 18.28 | 2.35 | » | 38.10 | 13.46 | 3.43 | 14.32 |
|  |  | 6.59 | 3.90 | 24.57 | 1.86 | » | 15.71 | 5.50 | 3.71 | 38.15 |
| o | 97.78 | 3.54 | 1.96 | 14.47 | 3.53 | » | 36.33 | 23.15 | 2.21 | 12.59 |
|  |  | 5.96 | 3.14 | 21.40 | 3.08 | » | 16.48 | 10.41 | 2.63 | 36.91 |
| n | 97.51 | 3.51 | 0.51 | 19.05 | 1.55 | » | 48.64 | 7.38 | 2.38 | 14.49 |
|  |  | 5.52 | 0.76 | 26.35 | 1.26 | » | 20.63 | 3.10 | 2.65 | 39.72 |
| Cu-Pd-Bi-S |  |  |  |  |  |  |  |  |  |  |
| n | 102.5 | 1.57 | 0.37 | 6.66 | 3.63 | 19.87 | b.d.l. | 67.87 | b.d.l. | 2.53 |
|  |  | 3.68 | 0.83 | 13.73 | 4.41 | 24.47 | » | 42.55 | » | 10.34 |
| o | 102.64 | 1.62 | 0.97 | 5.32 | 3.65 | 22.42 | » | 66.16 | » | 2.51 |
|  |  | 3.77 | 2.15 | 10.89 | 4.40 | 27.41 | » | 41.19 | » | 10.19 |
| o | 96.97 | 6.52 | 3.46 | 31.12 | 5.09 | 10.47 | » | 25.64 | 0.97 | 13.70 |
|  |  | 8.50 | 4.29 | 35.66 | 3.44 | 7.17 | » | 8.93 | 0.89 | 31.12 |
| o | 98.96 | 7.15 | 5.27 | 28.79 | 0.51 | 13.04 | » | 28.79 | 1.06 | 14.35 |
|  |  | 9.16 | 6.43 | 32.43 | 0.34 | 8.77 | » | 9.86 | 0.96 | 32.04 |
| i | 96.9 | 6.20 | 0.60 | 33.54 | 4.42 | 13.03 | » | 24.61 | 1.13 | 13.38 |
|  |  | 8.15 | 0.75 | 38.76 | 3.01 | 8.99 | » | 8.65 | 1.05 | 30.64 |
| Cu-Ag-Bi-Pb-As-S3 |  |  |  |  |  |  |  |  |  |  |
| i | 99.41 | 2.21 | 0.34 | 19.4 | 9.13 | b.d.l. | 19.37 | 24.35 | 2.05 | 17.31 |
|  |  | 3.09 | 0.45 | 23.83 | 6.61 | » | 7.30 | 9.09 | 2.03 | 42.14 |
| Cu-Ag-Pb-S |  |  |  |  |  |  |  |  |  |  |
| j | 103.73 | 5.32 | 0.27 | 24.25 | 14.78 | » | 32.12 | 10.54 | 2.44 | 14.01 |
|  |  | 7.37 | 0.36 | 29.54 | 10.61 | » | 12.00 | 3.90 | 2.39 | 33.83 |
| Ag-Pb-Bi-S |  |  |  |  |  |  |  |  |  |  |
| k | 99.41 | 0.33 | 0.30 | 4.47 | 16.39 | » | 31.59 | 30.23 | 2.82 | 13.28 |
|  |  | 0.6 | 0.52 | 7.18 | 15.5 | » | 15.55 | 14.76 | 3.64 | 42.25 |
| g | 101.08 | 0.28 | b.d.l. | 4.58 | 17.47 | » | 29.76 | 31.93 | 2.63 | 14.43 |
|  |  | 0.49 | » | 7.07 | 15.90 | » | 14.10 | 15.00 | 3.27 | 44.18 |
| Ag-Ni-Bi-S |  |  |  |  |  |  |  |  |  |  |
| n | 106.18 | 1.23 | 13.68 | 5.67 | 28.28 | » | 13.04 | 35.3 | 1.41 | 7.57 |
|  |  | 2.02 | 21.34 | 8.17 | 24.00 | » | 5.76 | 15.46 | 1.63 | 21.62 |

Note. Compositions expressed in wt. % and in at. % are in the first and second rows for each phase, respectively; b.d.l. – below detection limit; 1 - the names of the systems are given according to the main components; 2- numbers of figures with microstructures of solid solutions of the Cu-Pb-Bi-S, Cu-Pd-Bi-S, Cu-Ag-Pb-S, Cu-Ag-Bi-Pb-As-S systems and phases of the Ag-Pb-Bi-S and Ag-Ni-Bi-S systems are indicated; 3 - the solid solution contains  5.25 wt. % (5.47 at. %) As.