Table S1. Representative compositions of sulfides from the Cu–Fe–S system at the Lazurnoe ore occurrence, wt. %

| № | Fe | Cu | Ag | S | Total |  | Formula |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 30,96 | 33,56 |  | 34,35 | 98,87 |  | Cu0.98Fe1.03S1.99 |
| 2 | 31,05 | 33,97 |  | 34,33 | 99,35 |  | Cu0.99Fe1.03S1.98 |
| 3 | 30,56 | 34,12 |  | 34,68 | 99,36 |  | Cu0.99Fe1.01S2.00 |
| 4 | 31,65 | 32,23 |  | 35,52 | 99,40 |  | Cu0.99Fe1.04S2.03 |
| 5 | 30,83 | 34,00 |  | 34,64 | 99,47 |  | Cu0.99Fe1.02S1.99 |
| 6 | 31,40 | 32,64 |  | 35,06 | 99,10 |  | Cu0.95Fe1.04S2.02 |
| 7 | 30,77 | 34,25 |  | 34,33 | 99,35 |  | Cu1.00Fe1.02S1.98 |
| 8 | 30,78 | 34,52 |  | 34,69 | 99,99 |  | Cu1.00Fe1.01S1.99 |
| 9 | 30,52 | 33,83 |  | 34,43 | 98,78 |  | Cu0.99Fe1.02S2.00 |
| 10 | 30,34 | 33,93 |  | 34,30 | 98,57 |  | Cu0.99Fe1.01S1.99 |
| 11 | 30,53 | 33,98 |  | 34,46 | 98,97 |  | Cu0.99Fe1.01S1.99 |
| 12 | 30,89 | 34,27 |  | 34,19 | 99,35 |  | Cu1.00Fe1.02S1.98 |
| 13 | 30,53 | 34,22 |  | 34,18 | 98,93 |  | Cu1.00Fe1.02S1.98 |
| 14 | 30,62 | 33,89 |  | 34,32 | 98,83 |  | Cu0.99Fe1.02S1.99 |
| 15 | 31,27 | 34,12 |  | 34,52 | 99,91 |  | Cu0.99Fe1.03S1.98 |
| 16 | 30,75 | 34,24 |  | 34,87 | 99,86 |  | Cu0.99Fe1.01S2.00 |
| 17 | 30,42 | 34,75 |  | 34,65 | 99,87 |  | Cu1.00Fe1.00S1.98 |
| 18 | 46,40 |  |  | 52,50 | 98,90 |  | Fe1.01S1.99 |
| 19 | 46,57 |  |  | 52,07 | 98,64 |  | Fe1.02S1.98 |
| 20 | 47,44 |  |  | 53,35 | 100,79 |  | Fe1.01S1.99 |
| 21 | 45,87 |  |  | 52,35 | 98,22 |  | Fe1.00S2.00 |
| 22 | 46,90 |  |  | 52,95 | 99,85 |  | Fe1.01S1.99 |
| 23 | 46,52 |  |  | 52,93 | 99,45 |  | Fe1.01S1.99 |
| 24 | 47,16 |  |  | 53,23 | 100,39 |  | Fe1.01S1.99 |
| 25 | 46,90 |  |  | 52,71 | 99,61 |  | Fe1.01S1.99 |
| 26 | 46,49 |  |  | 52,62 | 99,11 |  | Fe1.01S1.99 |
| 27 | 10,35 | 63,26 |  | 23,88 | 97,49 |  | Cu5.17Fe0.96S3.87 |
| 28 | 18,27 | 62,85 |  | 30,24 | 101,36 |  | Cu3.96Fe1.56S4.49 |
| 29 | 16,65 | 54,96 | 0,53 | 28,91 | 101,05 |  | (Cu4.18Ag0.02)Σ4.20Fe1.44S4.36 |
| 30 | 16,91 | 53,37 | 1,20 | 27,34 | 98,82 |  | (Cu4.19Ag0.06)Σ4.26Fe1.51S4.25 |

1–17 – chalcopyrite CuFeS2; 18–26 – pyrite FeS2; 27–30 – bornite Cu5FeS4. An empty cell indicates an element concentration below the detection limit (applies throughout). Compositions for Figure 8.

Table S2. Compositions of galena, matildite, and sphalerite from the Lazurnoe ore occurrence, wt %

| № | Zn | Ag | Cd | Pb | Bi | Se | S | Total | Formula |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  |  |  | 87,05 |  |  | 12,44 | 99,49 | Pb1.04S0.96 |
| 2 |  |  |  | 87,05 |  |  | 12,45 | 99,50 | Pb1.04S0.96 |
| 3 |  |  |  | 86,94 |  |  | 12,44 | 99,38 | Pb1.04S0.96 |
| 4 |  |  |  | 87,30 |  |  | 12,53 | 99,83 | Pb1.04S0.96 |
| 5 |  |  |  | 87,42 |  |  | 12,57 | 99,99 | Pb1.04S0.96 |
| 6 |  |  |  | 87,35 |  |  | 12,58 | 99,93 | Pb1.04S0.96 |
| 7 |  |  |  | 87,57 |  |  | 12,62 | 100,19 | Pb1.04S0.96 |
| 8 |  |  |  | 86,39 |  |  | 12,48 | 98,87 | Pb1.03S0.97 |
| 9 |  |  |  | 86,13 |  |  | 12,47 | 98,60 | Pb1.03S0.97 |
| 10 |  |  |  | 86,62 |  |  | 12,56 | 99,18 | Pb1.03S0.97 |
| 11 |  |  |  | 86,32 |  |  | 12,55 | 98,87 | Pb1.03S0.97 |
| 12 |  |  |  | 86,19 |  |  | 12,55 | 98,74 | Pb1.03S0.97 |
| 13 |  |  |  | 86,72 |  |  | 12,64 | 99,36 | Pb1.03S0.97 |
| 14 |  |  |  | 86,88 |  |  | 12,96 | 99,84 | Pb1.02S0.98 |
| 15 |  |  |  | 84,09 | 2,98 |  | 12,97 | 100,04 | (Pb0.98Bi0.03)Σ1.01S0.99 |
| 16 |  |  |  | 84,59 | 3,04 |  | 12,81 | 100,44 | (Pb0.99Bi0.04)Σ1.03S0.97 |
| 17 |  |  |  | 83,90 | 3,10 |  | 12,52 | 99,52 | (Pb1.00Bi0.04)Σ1.04S0.96 |
| 18 |  |  |  | 85,77 |  | 1,11 | 12,30 | 99,18 | Pb1.02(S0.95Se0.03)Σ0.98 |
| 19 |  |  |  | 84,58 |  | 3,33 | 11,09 | 99,00 | Pb1.03(S0.87Se0.11)Σ0.98 |
| 20 |  |  |  | 85,10 |  | 1,82 | 11,86 | 98,78 | Pb1.02(S0.92Se0.06)Σ0.98 |
| 21 |  |  |  | 84,72 |  | 3,66 | 11,14 | 99,52 | Pb1.02(S0.87Se0.12)Σ0.99 |
| 22 |  |  |  | 84,84 |  | 1,96 | 11,87 | 98,67 | Pb1.02(S0.92Se0.06)Σ0.98 |
| 23 |  |  |  | 83,49 |  | 3,12 | 11,69 | 98,30 | Pb1.00(S0.90Se0.10)Σ01.00 |
| 24 |  |  |  | 83,46 |  | 2,43 | 12,67 | 98,56 | Pb0.97(S0.95Se0.07)Σ1.02 |
| 25 |  |  |  | 83,50 | 2,83 | 1,23 | 12,39 | 99,95 | (Pb0.98Bi0.03)Σ1.01(S0.94Se0.04)Σ0.98 |  |
| 26 |  |  |  | 80,85 | 3,81 | 3,67 | 11,06 | 99,39 | (Pb0.98Bi0.05)Σ1.03(S0.86Se0.12)Σ0.98 |  |
| 27 |  |  |  | 76,84 | 7,38 | 1,81 | 12,65 | 98,68 | (Pb0.90Bi0.09)Σ0.99(S0.96Se0.06)Σ1.02 |  |
| 28 |  | 3,82 |  | 77,48 |  | 4,62 | 10,59 | 96,51 | (Pb0.94Ag0.09)Σ1.03(S0.83Se0.15)Σ0.98 |  |
| 29 |  | 1,26 |  | 78,85 |  | 7,94 | 9,05 | 97,10 | (Pb0.98Ag0.03)Σ1.01(S0.73Se0.26)Σ0.99 |  |
| 30 |  | 1,73 |  | 78,93 |  | 2,84 | 11,72 | 95,22 | (Pb0.95Ag0.04)Σ0.99(S0.92Se0.09)Σ1.01 |  |
| 31 |  | 3,30 |  | 73,63 | 6,24 | 3,54 | 11,36 | 98,07 | (Pb0.87Ag0.08Bi0.07)Σ1.02(S0.87Se0.11)Σ0.98 |  |
| 32 |  | 5,10 |  | 73,18 | 3,17 | 3,13 | 13,70 | 98,28 | (Pb0.80Ag0.11Bi0.03)Σ0.94(S0.97Se0.09)Σ1.06 |  |
| 33 |  | 2,65 |  | 78,29 | 3,35 | 2,25 | 12,25 | 98,79 | (Pb0.91Ag0.06Bi0.04)Σ1.01(S0.92Se0.07)Σ0.99 |  |
| 34 |  | 5,70 |  | 70,22 | 7,03 | 5,04 | 11,21 | 99,20 | (Pb0.81Ag0.13Bi0.08)Σ1.02(S0.83Se0.15)Σ0.98 |  |
| 35 |  | 4,33 |  | 72,68 | 7,01 | 4,62 | 10,87 | 99,51 | (Pb0.85Ag0.10Bi0.08)Σ1.03(S0.82Se0.14)Σ0.96 |  |
| 36 |  | 3,26 |  | 76,59 | 4,55 | 2,80 | 12,41 | 99,61 | (Pb0.88Ag0.07Bi0.05)Σ1.00(S0.92Se0.08)Σ1.00 |  |
| 37 |  | 2,69 |  | 78,70 | 3,67 | 2,74 | 11,88 | 99,68 | (Pb0.92Ag0.06Bi0.04)Σ1.02(S0.90Se0.08)Σ0.98 |  |
| 38 |  | 4,29 |  | 72,53 | 7,25 | 5,12 | 10,74 | 99,93 | (Pb0.85Ag0.10Bi0.08)Σ1.03(S0.81Se0.16)Σ0.97 |  |
| 39 |  | 1,80 |  | 81,02 | 3,51 | 2,45 | 12,02 | 100,80 | (Pb0.94Ag0.04Bi0.04)Σ1.02(S0.90Se0.07)Σ0.97 |  |  |
| 40 |  | 20,99 |  | 24,58 | 33,62 | 3,36 | 13,21 | 95,76 | Ag0.84(Bi0.69Pb0.51)Σ1.20(S1.77Se0.18)Σ1.95 |  |  |
| 41 |  | 26,02 |  | 12,00 | 40,58 | 1,99 | 14,32 | 94,91 | Ag1.00(Bi0.80Pb0.24)Σ1.04(S1.85Se0.10)Σ1.95 |  |  |
| 42 |  | 21,01 |  | 25,70 | 34,74 | 2,16 | 14,22 | 97,83 | Ag0.82(Bi0.70Pb0.52)Σ1.22(S1.86Se0.11)Σ1.97 |  |  |
| 43 |  | 27,22 |  |  | 50,94 | 2,48 | 15,7 | 96,34 | Ag0.99Bi0.96(S1.93Se0.12)Σ2.05 |  |  |
| 44 |  | 26,76 |  |  | 49,61 | 2,89 | 15,06 | 94,32 | Ag1.00Bi0.96(S1.89Se0.15)Σ2.04 |  |  |
| 45 |  | 7,59 |  | 57,33 | 11,74 | 2,28 | 12,88 | 91,82 | (Pb0.66Ag0.17Bi0.13)Σ0.96(S0.97Se0.07)Σ1.04 |  |  |
| 46 | 62,32 |  | 0,99 |  |  |  | 32,86 | 96,17 | (Zn0.96Cd0.01)Σ0.97S1.03 |  |  |
| 47 | 62,23 |  | 1,43 |  |  |  | 33,86 | 97,52 | (Zn0.94Cd0.01)Σ0.95S1.05 |  |  |
| 48 | 65,47 |  | 0,81 |  |  |  | 32,63 | 98,91 | (Zn0.99Cd0.01)Σ1.00S1.00 |  |  |

1-17 – gold-hessite-galena association; 18-48 – sulfosalt-acanthite-chalcopyrite association: 1-14 – galena PbS; 15-17 – Bi-galena (Pb,Bi)S; 18-24 – Se-galena Pb(S,Se); 25-27 – Se and Bi-galena (Pb,Bi)(S,Se); 28-30 – Ag and Se-galena (Pb,Ag)(S,Se); 31-39 – Bi, Ag and Se-galena (Pb,Bi,Ag)(S,Se); 40-44 – matildite AgBiS2; 45 – galena-matildite solid solution (Pb,Ag,Bi)(S,Se);  46-48 – Cd-sphalerite (Zn,Cd)S. Compositions for Figure 9.

Table S3. Representative compositions of solid solutions of the acanthite series and other minerals of the Ag(+Cu,Fe)–S–Se system from the Lazurnoe ore occurrence, wt. %.

| № п/п | Fe | Cu | Ag | Te | Se | S | Total | Formula |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2,25 | 1,51 | 83,18 |  |  | 12,61 | 99,55 | (Ag1.88Fe0.10Cu0.06)Σ2.04S0.96 |
| 2 | 0,54 | 4,29 | 82,04 |  |  | 12,91 | 99,78 | (Ag1.84Cu0.16Fe0.02)Σ2.03S0.97 |
| 3 | 0,82 | 2,56 | 83,12 |  |  | 13,84 | 100,34 | (Ag1.84Cu0.10Fe0.04)Σ1.97S1.03 |
| 4 | 2,92 | 0,45 | 81,76 | 0,52 | 1,38 | 12,09 | 99,12 | (Ag1.87Fe0.13Cu0.02)Σ2.02(S0.93Se0.04Te0.01)Σ0.98 |
| 5 | 1,39 | 0,51 | 82,56 |  | 1,60 | 12,43 | 98,49 | (Ag1.90Fe0.06Cu0.02)Σ1.99(S0.96Se0.05)Σ1.01 |
| 6 | 1,95 | 3,83 | 79,94 |  | 2,50 | 10,89 | 99,11 | (Ag1.84Cu0.15Fe0.09)Σ2.08(S0.84Se0.08)Σ0.92 |
| 7 | 2,34 |  | 82,24 |  | 3,27 | 10,52 | 98,37 | (Ag1.95Fe0.11)Σ2.06(S0.84Se0.11)Σ0.94 |
| 8 | 0,35 | 1.00 | 79,75 | 1,01 | 7,53 | 8,88 | 98,52 | (Ag1.94Cu0.04Fe0.02)Σ2.00(S0.73Se0.25Te0.02)Σ1.00 |
| 9 | 1,77 | 5,69 | 72,78 | 1,82 | 10,14 | 7,06 | 99,26 | (Ag1.75Cu0.23Fe0.08)Σ2.06(S0.57Se0.33Te0.04)Σ0.94 |
| 10 | 1,98 | 5,16 | 73,14 |  | 11,79 | 6,09 | 98,16 | (Ag1.79Cu0.21Fe0.09)Σ2.10(S0.50Se0.40)Σ0.90 |
| 11 | 1,30 | 4,77 | 75,39 | 0,52 | 12,18 | 6,63 | 100,79 | (Ag1.80Cu0.19Fe0.06)Σ2.06(S0.53Se0.40Te0.01)Σ0.94 |
| 12 | 1,21 | 5,37 | 72,47 | 1,50 | 12,36 | 5,87 | 98,78 | (Ag1.78Cu0.22Fe0.06)Σ2.07(S0.49Se0.42Te0.03)Σ0.93 |
| 13 | 1,06 | 6,08 | 71,57 | 1,82 | 14,02 | 5,95 | 100,50 | (Ag1.72Cu0.25Fe0.05)Σ2.02(S0.48Se0.46Te0.04)Σ0.98 |
| 14 | 1,90 | 7,76 | 71,15 |  | 14,64 | 5,81 | 101,26 | (Ag1.67Cu0.31Fe0.09)Σ2.07(Se0.47S0.46)Σ0.93 |
| 15 | 1,88 | 2,51 | 75,34 | 1,39 | 14,74 | 4,56 | 100,42 | (Ag1.89Cu0.11Fe0.09)Σ2.08(Se0.50S0.38Te0.03)Σ0.92 |
| 16 | 2,00 | 9,31 | 67,02 | 0,61 | 15,70 | 6,49 | 101,13 | (Ag1.54Cu0.36Fe0.09)Σ1.99(S0.50Se0.49Te0.01)Σ1.01 |
| 17 | 1,15 | 9,76 | 68,44 |  | 16,15 | 6,16 | 101,66 | (Ag1.58Cu0.38Fe0.05)Σ2.01(Se0.51S0.48)Σ0.99 |
| 18 | 1,35 | 8,06 | 69,72 | 0,77 | 16,49 | 5,46 | 101,85 | (Ag1.64Cu0.32Fe0.06)Σ2.02(Se0.53S0.43Te0.02)Σ0.98 |
| 19 | 1,53 | 8,27 | 67,40 | 0,92 | 16,78 | 4,12 | 99,02 | (Ag1.66Cu0.35Fe0.07)Σ2.08(Se0.56S0.34Te0.02)Σ0.92 |
| 20 | 0,72 | 2.00 | 75,85 | 1,45 | 16,8 | 4,04 | 100,86 | (Ag1.92Cu0.09Fe0.04)Σ2.04(Se0.58S0.34Te0.03)Σ0.96 |
| 21 | 2,45 | 1,45 | 71,37 | 2,82 | 19,44 | 1,69 | 99,22 | (Ag1.89Fe0.13Cu0.07)Σ2.08(Se0.70S0.15Te0.06)Σ0.92 |
| 22 | 2,31 | 2,52 | 71,86 | 0,94 | 20,73 | 1,80 | 100,16 | (Ag1.86Fe0.12Cu0.11)Σ2.09(Se0.73S0.16Te0.02)Σ0.91 |
| 23 | 1,74 | 22,52 | 57,74 |  |  | 14,01 | 96,01 | Ag4.73(Cu3.13Fe0.28)Σ3.41S3.86 |
| 24 | 0,66 | 26,05 | 48,15 | 0,83 | 13,19 | 7,72 | 96,60 | Ag1.04(Cu0.96Fe0.03)Σ0.99(S0.56Se0.39Te0.02)Σ0.97 |
| 25 | 2,27 | 27,23 | 49,76 |  | 5,70 | 12,86 | 97,82 | Ag0.99(Cu0.92Fe0.09)Σ1.01(S0.86Se0.15)Σ1.01 |
| 26 | 1,23 | 11,45 | 66,37 | 0,82 | 13,07 | 6,89 | 99,83 | Ag3.07(Cu0.90Fe0.11)Σ1.01(S1.07Se0.82Te0.03)Σ1.93 |
| 27 | 1,95 | 10,08 | 68,52 | 1,71 | 10,66 | 8,35 | 101,27 | Ag3.08(Cu0.77Fe0.17)Σ0.94(S1.26Se0.65Te0.06)Σ1.98 |
| 28 | 0,76 | 33,78 | 47,35 |  | 4,80 | 13,89 | 100,58 | (Cu1.08Fe0.03)Σ1.11Ag0.89(S0.88Se0.12)Σ1.00 |
| 29 | 3,37 | 31,14 | 45,07 |  | 12,30 | 9,96 | 101,84 | (Cu1.02Fe0.13)Σ1.15Ag0.87(S0.65Se0.33)Σ0.98 |
| 30 | 1,47 | 39,06 | 39,01 |  | 3,06 | 15,31 | 97,91 | (Cu1.21Fe0.05)Σ1.26Ag0.71(S0.94Se0.08)Σ1.02 |
| 31 | 5,24 | 36,09 | 35,95 | 1,01 | 9,14 | 12,79 | 100,22 | (Cu1.12Fe0.19)Σ1.31Ag0.66(S0.79Se0.23)Σ1.03 |
| 32 | 3,11 | 41,57 | 37,96 |  | 1,96 | 15,90 | 100,50 | (Cu1.24Fe0.11)Σ1.35Ag0.67(S0.94Se0.05)Σ0.99 |
| 33 | 1,25 | 45,10 | 35,17 |  | 2,39 | 16,16 | 100,07 | (Cu1.34Fe0.04)Σ1.38Ag0.61(S0.95Se0.06)Σ1.01 |
| 34 | 3,39 | 58,78 | 15,82 |  | 5,56 | 18.00 | 101,55 | (Cu1.57Fe0.10)Σ1.67Ag0.25(S0.95Se0.12)Σ1.07 |
| 35 | 1,71 | 55,77 | 22,57 |  | 2,58 | 17,92 | 100,55 | (Cu1.54Fe0.05)Σ1.59Ag0.37(S0.98Se0.06)Σ1.04 |
| 35 | 1,60 | 48,18 | 30,40 |  | 3,55 | 16,61 | 100,34 | (Cu1.39Fe0.05)Σ1.44Ag0.52(S0.95Se0.08)Σ1.04 |

1-20 – Cu- and Fe-bearing minerals of the acanthite series (Ag,Cu,Fe)2(S,Se); 21,22 – naumannite Ag2Se; 23 – the mineral similar in composition to mckinstryite Ag6Cu3S4; 24, 25 – stromeyerite CuAg(S,Se); 26, 27 – yalpaite Ag3CuS2; 28-35 – finely dispersed mixture of chalcocite minerals Cu2S and acanthite Ag2S.  Compositions for Figure 10.

Table S4. Compositions of tetrahedrite-group sulfosalts with the general formula Cu6[Cu4(Zn,Fe)2](Sb,As,Bi)4S13 from the Lazurnoe ore occurrence, wt.%

| № | Fe | Cu | Zn | Ag | Bi | Sb | As | S | Total | Formula |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2,63 | 41,22 | 7,303 |  |  | 11,62 | 10,93 | 27,27 | 101,00 | Cu6.00(Cu3.90Zn1.71Fe0.72)Σ6.33(As2.23Sb1.46)Σ3.69S12.98 |
| 2 | 2,08 | 41,41 | 7,50 |  |  | 9,40 | 13,15 | 26,84 | 100,38 | Cu6.00(Cu3.98Zn1.76Fe0.57)Σ5.31(As2.69Sb1.18)Σ3.87S12.82 |
| 3 | 2,66 | 40,86 | 6,97 |  |  | 10,68 | 11,50 | 26,75 | 99,42 | Cu6.00(Cu3.96Zn1.65Fe0.74)Σ6.35(As2.38Sb1.36)Σ3.74S12.92 |
| 4 | 2,43 | 41,00 | 7,48 |  |  | 9,08 | 13,07 | 26,73 | 99,79 | Cu6.00(Cu3.92Zn1.76Fe0.67)Σ6.35(As2.68Sb1.15)Σ3.83S12.82 |
| 5 | 2,45 | 41,62 | 7,48 |  |  | 7,65 | 13,55 | 27,06 | 99,81 | Cu6.00(Cu3.99Zn1.75Fe0.67)Σ6.41(As2.76Sb0.96)Σ3.72S12.88 |
| 6 | 2,58 | 42,33 | 6,96 |  |  | 5,65 | 14,98 | 27,23 | 99,73 | Cu6.00(Cu4.09Zn1.61Fe0.70)Σ6.40(As3.03Sb0.70)Σ3.73S12.86 |
| 7 | 2,52 | 43,96 | 5,65 |  |  | 2,72 | 16,97 | 27,82 | 99,64 | Cu6.00(Cu4.34Zn1.29Fe0.67)Σ6.30(As3.39Sb0.33)Σ3.72S12.97 |
| 8 | 3,79 | 41,05 | 6,91 |  |  | 5,32 | 13,68 | 27,47 | 98,22 | Cu6.00(Cu3.85Zn1.61Fe1.03)Σ6.49(As2.78Sb0.67)Σ3.45S13.06 |
| 9 | 2,17 | 45,17 | 5,91 |  |  |  | 18,96 | 28,46 | 100,67 | Сu6.00(Cu4.41Zn1.32Fe0.57)Σ6.30As3.71S13.00 |
| 10 | 2,23 | 42,80 | 6,66 | 0,52 |  | 0,39 | 18,56 | 27,74 | 98,90 | (Cu5.93Ag0.07)Σ6.00(Cu4.16Zn1.53Fe0.60)Σ6.29(As3.71Sb0.05)Σ3.76S12.96 |
| 11 | 2,67 | 41,75 | 6,57 | 3,36 |  | 0,70 | 17,55 | 27,31 | 99,91 | (Cu5.53Ag0.47)Σ6.00(Cu4.35Zn1.51Fe0.72)Σ6.23(As3.52Sb0.09)Σ3.61S12.81 |
| 12 | 5,93 | 39,88 | 6,48 | 1,08 |  | 4,89 | 13,27 | 28,14 | 99,67 | (Cu5.85Ag0.15)Σ6.00(Cu3.54Zn1.48Fe1.59)Σ6.61(As2.65Sb0.60)Σ3.25S13.13 |
| 13 | 2,98 | 42,28 | 7,22 | 1,08 |  |  | 17,73 | 27,38 | 98,67 | (Cu5.85Ag0.15)Σ6.00(Cu4.15Zn1.66Fe0.80)Σ6.61As3.56S12.83 |
| 14 | 5,22 | 40,49 | 6,93 |  |  | 0,41 | 16,90 | 28,45 | 98,40 | Cu6.00(Cu3.46Zn1.57Fe1.39)Σ6.42(As3.35Sb0.05)Σ3.40S13.18 |
| 15 | 3,55 | 43,01 | 6,81 |  |  |  | 17,17 | 28,28 | 98,82 | Cu6.00(Cu4.04Zn1.54Fe0.94)Σ6.52As3.40S13.08 |
| 16 | 4,68 | 43,76 | 6,41 | 0,55 |  | 0,42 | 16,46 | 26,80 | 99,08 | (Cu5.92Ag0.08)Σ6.00(Cu4.40Zn1.47Fe1.26)Σ7.13(As3.29Sb0.05)Σ3.35S12.53 |
| 17 | 4,46 | 39,62 | 6,99 |  |  | 6,95 | 12,49 | 27,71 | 98,22 | Cu6.00(Cu3.53Zn1.63Fe1.22)Σ6.38(As2.55Sb0.87)Σ3.42S13.20 |
| 18 | 6,30 | 41,80 | 6,18 |  |  | 0,42 | 15,75 | 28,93 | 99,38 | Cu6.00(Cu3.63Fe1.65Zn1.38)Σ6.66(As3.08Sb0.05)Σ3.13S13.21 |
| 19 | 6,42 | 42,32 | 5,73 |  |  | 1,46 | 15,20 | 28,75 | 99,88 | Cu6.00(Cu3.75Fe1.68Zn1.28)Σ6.71(As2.97Sb0.18)Σ3.15S13.13 |
| 20 | 6,57 | 39,78 | 6,44 |  |  | 5,23 | 13,11 | 28,04 | 99,17 | Cu6.00(Cu3.38Fe1.76Zn1.48)Σ6.62(As2.62Sb0.64)Σ3.27S13.11 |
| 21 | 7,62 | 40,15 | 6,07 |  |  |  | 15,93 | 29,64 | 99,41 | Cu6.00(Cu3.17Fe1.98Zn1.35)Σ6.50As3.09S13.42 |
| 22 | 8,43 | 41,68 | 5,68 |  |  | 0,45 | 14,63 | 29,55 | 100,42 | Cu6.00(Cu3.44Fe2.17Zn1.25)Σ6.86(As2.81Sb0.05)Σ2.86S13.27 |
| 23 | 10,30 | 38,48 | 5,76 |  |  | 6,03 | 10,52 | 28,55 | 99,64 | Cu6.00(Cu2.97Fe2.73Zn1.30)Σ7.00(As2.08Sb0.73)Σ2.81S13.18 |
| 24 | 12,23 | 39,44 | 5,20 |  |  | 0,86 | 12,63 | 30,59 | 100,95 | Cu6.00(Cu2.78(Fe3.10Zn1.13)Σ7.01(As2.39Sb0.10)Σ2.49S13.50 |
| 25 | 10,11 | 36,24 | 5,17 | 1,21 | 3,33 | 0,36 | 11,65 | 29,27 | 97,34 | (Cu5.83Ag0.17)Σ6.00(Cu2.74Fe2.72Zn1.19)Σ6.65(As2.34Bi0.24Sb0.04)Σ2.62S13.72 |
| 26 | 4,91 | 37,48 | 6,67 |  | 7,81 | 8,25 | 8,40 | 26,21 | 99,73 | Cu6.00(Cu3.49Zn1.63Fe1.41)Σ6.52(As1.76Sb1.08Bi0.60)Σ3.47S13.06 |
| 27 | 5,72 | 38,02 | 6,07 |  | 9,12 | 4,65 | 9,77 | 26,75 | 100,00 | Cu6.00(Cu3.43Fe1.61Zn1.46)Σ6.50(As2.06Bi0.69Sb0.60)Σ3.35S13.15 |
| 28 | 2,72 | 37,89 | 6,65 |  | 12,91 | 4,55 | 9,78 | 25,34 | 99,84 | Cu6.00(Cu3.79Zn1.67Fe0.80)Σ6.26(As2.14Bi1.01Sb0.61)Σ3.77S12.97 |
| 29 | 1,95 | 36,34 | 6,79 |  | 15,45 | 6,15 | 6,78 | 23,90 | 97,36 | Cu6.00(Cu3.92Zn1.80Fe0.61)Σ6.33(As1.57Bi1.28Sb0.88)Σ3.73S12.94 |
| 30 | 2,50 | 35,56 | 6,45 |  | 17,24 | 6,29 | 6,01 | 23,13 | 97,18 | Cu6.00(Cu3.90Zn1.75Fe0.79)Σ6.44(Bi1.46As1.42Sb0.91)Σ3.79S12.77 |
| 31 | 4,24 | 34,88 | 6,33 |  | 18,58 | 6,50 | 5,00 | 23,96 | 99,49 | Cu6.00(Cu3.49Zn1.67Fe1.31)Σ6.47(Bi1.54As1.15Sb0.92)Σ3.61S12.91 |
| 32 | 2,19 | 38,07 | 7,24 |  |  | 26,48 | 2,61 | 24,24 | 99,73 | Cu6.00(Cu3.94Zn1.84Fe0.66)Σ6.44(Sb3.47As0.66)Σ4.03S12.64 |
| 33 | 1,66 | 38,04 | 7,63 |  |  | 24,31 | 2,86 | 24,63 | 98,93 | Cu6.00(Cu3.93Zn1.91Fe0.46)Σ6.30(Sb3.31As0.63)Σ3.94S12.76 |
| 34 | 2,46 | 39,02 | 7,36 |  |  | 19,69 | 6,99 | 26,62 | 100,13 | Cu6.00(Cu3.83Zn1.80Fe0.71)Σ6.44(Sb2.69As1.28)Σ3.87S12.79 |
| 35 | 1,71 | 39,18 | 7,00 |  |  | 19,02 | 7,16 | 26,74 | 99,80 | Cu6.00(Cu3.89Zn1.72Fe0.49)Σ6.10(Sb2.60As1.63)Σ4.03S12.87 |
| 36 | 1,97 | 39,36 | 6,97 |  |  | 18,61 | 7,29 | 26,86 | 101,00 | Cu6.00(Cu3.71Zn1.67Fe0.66)Σ6.04(Sb2.40As1.63)Σ3.93S13.14 |
| 37 | 7,14 | 38,67 | 6,61 |  |  | 16,06 | 6,21 | 27,29 | 100,80 | Cu6.00(Cu3.30(Fe1.96Zn1.66)Σ6.92(Sb1.89As1.27)Σ3.16S13.03 |

1-17 – tennantite-(Zn); 18-24 – tennantite-(Fe); 25-29 – Bi-rich variety tennantite-(Zn); 30,31 – Bi-analogue of tennantite-(Zn)»; 32-36 – tetrahedrite-(Zn);

40 – tetrahedrite-(Fe). To Figure 11.

Table S5. Compositions of minerals of the pearceite group from the Lazurnoe ore occurrence, wt. %

| № | Fe | Cu | Zn | Ag | Sb | Te | As | Se | S | Total | Formula |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1,75 | 35,87 | 2,42 | 28,93 | 3,16 |  | 4,50 | 7,05 | 17,16 | 100,84 | [Cu6.00(As1.08Sb0.47)Σ1.55S7.00][Ag4.83(Cu4.16Zn0.67Fe0.56)Σ5.39(S2.63Se1.61)Σ4.24] |
| 2 | 1,79 | 29,48 |  | 39,22 |  |  | 8,40 |  | 19,76 | 98,65 | [Cu6.00As2.05S7.00][Ag6.64(Cu2.47Fe0.59)Σ3.06S4.25] |
| 3 | 1,60 | 29,82 |  | 40,14 |  |  | 8,03 |  | 19,55 | 99,14 | [Cu6.00As1.96S7.00][Ag6.80(Cu2.58Fe0.52)Σ3.10S4.14] |
| 4 | 2,33 | 28,45 |  | 45,49 |  |  | 6,35 |  | 18,71 | 101,33 | [Cu6.00As1.56S7.00][Ag7.74(Cu2.22Fe0.77)Σ2.99S3.71] |
| 5 | 1,61 | 23,14 |  | 48,74 |  |  | 7,37 |  | 17,61 | 98,47 | [Cu6.00As1.91S7.00][Ag8.78(Cu1.08Fe0.56)Σ1.64S3.67] |
| 6 | 1,55 | 23,51 |  | 49,67 |  |  | 6,95 |  | 17,74 | 99,42 | [Cu6.00As1.79S7.00][Ag8.88(Cu1.13Fe0.54)Σ1.67S3.67] |
| 7 | 1,06 | 22,85 |  | 49,63 |  |  | 6,69 |  | 17,85 | 98,08 | [Cu6.00As1.74S7.00][Ag8.99(Cu1.02Fe0.37)Σ1.39S3.87] |
| 8 | 1,62 | 22,21 |  | 49,43 | 1,42 | 0,49 | 6,22 |  | 17,41 | 98,80 | [Cu6.00(As1.63Sb0.23Te0.08)Σ1.94S7.00][Ag8.99(Cu0.86Fe0.57)Σ1.43S3.65] |
| 9 | 1,39 | 22,45 |  | 50,55 | 1,20 |  | 6,25 |  | 17,75 | 99,59 | [Cu6.00(As1.62Sb0.19)Σ1.81S7.00][Ag9.10(Cu0.86Fe0.48)Σ1.34S3.75] |
| 10 | 1,13 | 18,15 |  | 58,49 |  |  | 6,13 |  | 16,94 | 100,84 | [(Cu5.68Fe0.40)Σ6.08As1.63S7.00][Ag10.78S3.51] |
| 11 | 2,99 | 10,96 |  | 64,29 | 4,45 |  | 2,81 |  | 16,01 | 101,51 | [(Cu3.58Fe1.11)Σ4.69(As0.78Sb0.76)Σ1.54S7.00][Ag12.39S3.38] |

1-8 - cupropirceite [Cu6As2S7][Ag9CuS4]; 9-11 – pearceite [Ag9CuS4][(Ag,Cu)6(As,Sb)2S7]. To Figure 12.

Table S6. Compositions of cervelleite and hessite from the Lazurnoe ore occurrence, wt %

| № п/п | Fe | Cu | Ag | Te | Se | S | Total | Formula |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1,22 | 8,98 | 62,14 | 21,23 | 2,22 | 5,41 | 101,20 | (Ag3.14Cu0.77Fe0.12)Σ4.02(S0.92Se0.15)Σ1.07Te0.91 |
| 2 | 0,81 | 8,43 | 62,38 | 22,04 | 1,71 | 5,66 | 101,03 | (Ag3.16Cu0.73Fe0.08)Σ3.97(S0.97Se0.12)Σ1.08Te0.95 |
| 3 | 1,99 | 5,67 | 63,78 | 21,44 | 2,18 | 5,44 | 100,50 | (Ag3.28Cu0.50Fe0.20)Σ3.97(S0.94Se0.15)Σ1.09Te0.93 |
| 4 | 1,13 | 6,27 | 63,32 | 19,67 | 2,83 | 5,14 | 98,36 | (Ag3.33Cu0.56Fe0.11)Σ4.01(S0.91Se0.20)Σ1.11Te0.88 |
| 5 | 1,71 | 8,05 | 61,45 | 21,39 | 1,96 | 5,06 | 99,62 | (Ag3.17Cu0.71Fe0.17)Σ4.05(S0.88Se0.14)Σ1.02Te0.93 |
| 6 | 2,62 | 10,26 | 58,39 | 18,28 | 2,28 | 6,75 | 98,58 | (Ag2.87Cu0.86Fe0.25)Σ3.97(S1.12Se0.15)Σ1.27Te0.76 |
| 7 | 1,05 | 12,08 | 59,23 | 17,06 | 3,54 | 6,57 | 99,53 | (Ag2.89Cu1.00Fe0.10)Σ3.98(S1.08Se0.24)Σ1.31Te0.70 |
| 8 | 1,13 | 8,31 | 63,18 | 21,16 | 1,38 | 6,13 | 101,29 | (Ag3.16Cu0.71Fe0.11)Σ3.98(S1.03Se0.09)Σ1.13Te0.90 |
| 9 | 1,86 | 13,35 | 58,79 | 18,31 | 2,23 | 7,03 | 101,57 | (Ag2.77Cu1.07Fe0.17)Σ4.01(S1.12Se0.14)Σ1.26Te0.73 |
| 10 |  |  | 63,09 | 36,22 |  |  | 99,31 | Ag2.02Te0.98 |
| 11 |  |  | 62,57 | 36,07 |  |  | 98,64 | Ag2.02Te0.98 |
| 12 |  |  | 62,83 | 35,95 |  | 0,21 | 98,99 | Ag2.01(Te0.97Se0.02)Σ0.99 |

1-9 – sulfosalt–acanthite–chalcopyrite association, cervelleite (Ag,Cu,Fe)4(S,Se)Te; 10-12 – gold–hessite–galena assemblage, hessite Ag2Te. To Figure 13.

Table S7. Compositions of native gold from the Lazurnoe ore occurrence

| № | Au | Ag | Total | Au | Ag | Total |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | wt. % |  |  | at. % |  |  |  |
| 1 | 96,48 | 2,61 | 98,99 | 96,46 | 4,64 | 100 |  |
| 2 | 96,90 | 2,99 | 99,89 | 94,67 | 6,33 | 100 |  |
| 3 | 96,76 | 3,04 | 99,80 | 94,67 | 6,43 | 100 |  |
| 4 | 96,91 | 3,06 | 99,96 | 94,67 | 6,43 | 100 |  |
| 5 | 96,14 | 3,16 | 99,30 | 94,34 | 6,66 | 100 |  |
| 6 | 96,14 | 3,36 | 99,60 | 94,00 | 6,00 | 100 |  |
| 7 | 96,86 | 3,39 | 99,26 | 93,93 | 6,07 | 100 |  |
| 8 | 94,89 | 3,60 | 98,39 | 93,69 | 6,31 | 100 |  |
| 9 | 94,78 | 3,67 | 98,36 | 93,66 | 6,44 | 100 |  |
| 10 | 96,26 | 3,71 | 99,96 | 93,42 | 6,68 | 100 |  |
| 11 | 96,14 | 3,76 | 99,90 | 93,33 | 6,67 | 100 |  |
| 12 | 94,67 | 4,76 | 99,33 | 91,68 | 8,42 | 100 |  |
| 13 | 93,71 | 6,77 | 99,48 | 89,89 | 10,11 | 100 |  |
| 14 | 92,69 | 6,07 | 98,66 | 89,31 | 10,69 | 100 |  |
| 15 | 93,62 | 6,16 | 99,67 | 89,28 | 10,72 | 100 |  |
| 16 | 92,6 | 6,18 | 98,78 | 89,14 | 10,86 | 100 |  |
| 17 | 92,41 | 6,26 | 98,66 | 89,01 | 10,99 | 100 |  |
| 18 | 92,26 | 7,06 | 99,31 | 87,76 | 12,24 | 100 |  |
| 19 | 90,46 | 9,36 | 99,81 | 84,11 | 16,89 | 100 |  |
| 20 | 89,07 | 9,32 | 98,39 | 83,96 | 16,04 | 100 |  |
| 21 | 88,72 | 9,48 | 98,20 | 83,67 | 16,33 | 100 |  |
| 22 | 88,71 | 10,40 | 99,11 | 82,37 | 17,63 | 100 |  |
| 23 | 89,03 | 10,66 | 99,69 | 82,20 | 17,80 | 100 |  |
| 24 | 87,36 | 11,19 | 98,66 | 81,04 | 18,96 | 100 |  |
| 25 | 87,86 | 11,29 | 99,16 | 81,00 | 19,00 | 100 |  |
| 26 | 87,41 | 11,27 | 98,68 | 80,94 | 19,06 | 100 |  |
| 27 | 88,07 | 11,37 | 99,44 | 80,92 | 19,08 | 100 |  |
| 28 | 87,96 | 11,64 | 99,49 | 80,67 | 19,33 | 100 |  |
| 29 | 87,33 | 11,60 | 98,93 | 80,48 | 19,62 | 100 |  |
| 30 | 87,82 | 11,69 | 99,61 | 80,46 | 19,66 | 100 |  |
| 31 | 87,64 | 12,06 | 99,69 | 79,93 | 20,07 | 100 |  |
| 32 | 86,46 | 11,96 | 98,42 | 79,83 | 20,17 | 100 |  |
| 33 | 86,31 | 11,98 | 98,29 | 79,78 | 20,22 | 100 |  |
| 34 | 86,55 | 12,38 | 98,93 | 79,29 | 20,71 | 100 |  |
| 35 | 85,97 | 12,42 | 98,39 | 79,13 | 20,87 | 100 |
| 36 | 83,91 | 14,84 | 98,75 | 75,59 | 24,41 | 100 |
| 37 | 71,96 | 27,64 | 99,60 | 58,78 | 41,22 | 100 |
| 38 | 70,85 | 29,11 | 99,96 | 57,13 | 42,87 | 100 |
| 39 | 67,88 | 31,99 | 99,87 | 53,75 | 46,25 | 100 |
| 40 | 41,3 | 57,46 | 98,76 | 28,24 | 71,76 | 100 |
| 41 | 39,84 | 59,17 | 99,01 | 26,94 | 73,06 | 100 |
| 42 | 38,39 | 60,17 | 98,56 | 25,89 | 74,11 | 100 |
| 43 | 36,52 | 61,91 | 98,43 | 24,42 | 75,58 | 100 |

To Figure 14.