Table 1S. Major impurity components and unit cell edges of the synthesized pyrites

| № sample. | Composition, mol.% |  |  | а, nm** |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Observed | Calculated (by equation 1) |  |
|  |  |  |  |  | сm=0.00016 | сV=dV=0.00037 |
|  | CoS2 | CuS2* | FeSe2 |  |  |  |
| 1 | 0.66 | 0.4 (60) | - | 0.54182 | 0.54179 | 0.54188 |
| 2 | 0.6 | 0.76 (100) | - | 0.54205 | 0.54184 | 0.54200 |
| 3 | 1.19 | 1.1(100) | - | 0.54225 | 0.54197 | 0.54220 |
| 4 | 0.44 | 0.6 (100) | 1.59 | 0.54253 | 0.54239 | 0.54251 |
| 5 | 1.26 | 1.22 (100) | - | 0.54223 | 0.54200 | 0.54225 |
| 6 | 0.76 | 0.77 (100) | - | 0.54221 | 0.54186 | 0.54203 |
| 7 | 0.58 | 0.56 (52) | - | 0.54183 | 0.54181 | 0.54193 |
| 8 | 0.73 | 1.37 (50) | 0.01 | 0.54200 | 0.54196 | 0.54225 |
| 9 | 0.59 | 0.76 (?) | 3.12 | 0.54274 | 0.54300 | 0.54316 |
| 10 | 1.14 | 1.39 (64) | 0.28 | 0.54222 | 0.54211 | 0.54240 |
| 11 | 0.9 | 0.85 (100) | - | 0.54212 | 0.54189 | 0.54207 |
| 12 | 0.99 | 0.98 (89) | 0.68 | 0.54234 | 0.54218 | 0.54238 |
| 13 | 0.85 | 1.75 (43) | - | 0.54202 | 0.54203 | 0.54240 |
| 14 | 1.15 | 1.09 (100) | 0.42 | 0.54240 | 0.54212 | 0.54235 |
| 15 | 0.52 | 0.69 (100) | 0.17 | 0.54224 | 0.54189 | 0.54203 |

*The values in parentheses are estimates of the structural fraction of the CuS₂ impurity (%). For sample 9, there is poor agreement between the observed unit cell edge and the calculated values, possibly due to non-uniform Se distribution.

**Coincide or neighbor values are highlighted in the same color.

Table 2S. Correlations between distribution and cocrystallization coefficients in the pyrite–hydrothermal solution system

| DTE – DTE/Fe | r |
| --- | --- |
| Co – Co/Fe | -0.11 |
| Ni – Ni/Fe | 0.16 |
| Cu – Cu/Fe | -0.03 |
| Mn – Mn/Fe | 0.1 |
| Pt – Pt/Fe | 0.15 |
| Zn – Zn/Fe | 0.71 |
| As – As/Fe | 0.62 |
| Pd – Pd/Fe | 0.67 |
| Au – Au/Fe | 0.6 |